- CHARACTERISTICS

The putty MASTIC 353 is a product at thick consistency, grey, pre-accelerated. It’s ready for use and advised for automotive reparations.

- Polyester putty pre-accelerated, polymerise at room temperature following addition of benzoyle peroxide.

- Flexible putty, permits a easy application with spatula or toothed comb

- Rapid cure: can be sanded very quickly.

- No problem of adhesion with metal.

- PROPERTIES

| LIQUID PUTTY |  | CAST PUTTY |  |
| --- | --- | --- | --- |
| Brookfield viscosity (ISO 2555 - 23°C - sp96) | 0.5 rpm : 3000 - 3500 (x 1000) cP 5 rpm: 1400 - 1900 (x1000) cP | Time before sanding (20°C - 2% PBO) | 15 - 20 minutes |
| Specific gravity (ICON 012 - 23°C) | 1.71 - 1.75 g/cm3 |  |  |
| No volatile content (ICON 003) | 85 - 90% |  |  |
| Gel time (ICON 002) (23°C - 2% PBO on 150 g) | 5 - 7 minutes |  |  |

- PACKAGING

Available in cans of 5 kg.

- APPLICATION ADVISES

Mix the peroxide well, never put under 1% or over 3%.

This putty must be very well mixed with peroxide.

- STORAGE CONDITIONS AND HANDLING

Storage life: MASTIC 353 is stable for 6 months from date of production. The product must be stored in original closed packaging at a temperature between 15°C and 25°C, away from direct sunlight.

It is the responsibility of the customer to assure that the product is used in good conditions overall before the date limitation mentioned on the keg.

This putty is subject to the Highly Flammable Liquids Regulations.